## Slide 1
Synthesis of aliphatic polyesters from methyl 12-hydroxystearate, a bio derived AB monomer
Yogesh R. Nevare, Devyanee J. Nemade and Swaminathan Sivaram*
Polymer Science and Engineering Division, CSIR- National
Chemical Laboratory, Dr. Homi Bhabha Road, Pune 411008, India
email id: s.sivaram@iiserpune.ac.in, yr.nevare@ncl.res.in
Objectives
Synthesis of Me 12-HS and Poly(methyl 12-hydroxy stearate) (Poly(Me 12-HS))
Commercial 12-HSA
Purified Me 12-HS
Commercial 12-HSA
(75 % purity) m.p. 77oC
m. p. 55-58oC (lit. 50-51oC)
1H NMR (500MHz) spectrum of purified 12-HSA in CDCl3
Purification of 12-HSA
DSC of the 12-HSA
To understand the scope and limitation of transesterifcation- polymerisation reaction of Me 12-HS using a monomer of high purity.
To prepare high purity 12-HSA monomer, either by crystallisation or hydrolysis of a cyclic dimer and examine its polyesterification reaction in melt.
To explore the feasibility of ROP of a cyclic dimer of 12-HSA.
To understand the importance of cyclic oligomer formation in such polymerisation.
Future Work
YRN acknowledges DST for INSPIRE fellowship and CSIR-NCL for facilities.
1H-NMR of Poly(Me 12-HS)
Cyclics begin to form even at early stages of transesterification. The concurrent formation of cyclics could restrict the efficient polymerization of this monomer.
Absence of unsaturation and the ratio of e/f peak is 2:1, indicates this is an AB monomer.
Cyclic Na+ adduct
Linear Na+ Adduct
Cyclic K+ adduct
Linear K+ adduct
Acknowledgement
a
a
b
b
c
c
d
d
e
e
f
f
c
b
Unsaturation
absent
1H-NMR (200 MHz) spectrum of sample 8 (180oC) (after 24 h) in CDCl3.
The degree of polymerization was calculated by integrating proton g with proton h.
References
Bawn, C. E. H.; Huglin, M. B. Polymer 1962, 3, 257.
Stempfle, F.; Ortmann, P.; Mecking, S. Chem. Rev. 2016, 116, 4597.
Granata, A.; Sauriol, F.; Perlin, AS. Can. J Chem. 1994, 72, 1684.
Purified 12-HSA
12-HSA dissoved in pet ether, decanted (4 time)
Recrystallization from ethyl acetate (4 times)
m.p. 82oC
The highest reported m.p. in the literature with purity of > 99% observed m.p 82oC1.
Synthesis cyclic dimer of 12-HSA and Poly(12-HSA)
The method of hydrolysing a cyclic dimer of 12-HSA may offer another method to generate monomer grade 12-HSA; additionally a ROP of the cyclic dimer using an appropriate catalyst may offer a method to directly make polymers of 12-HSA.
1H-NMR of Cyclic dimer of 12-HSA
Disappearance of peak at 3.59 ppm due to the linear chain indicate that the formation of cyclic dimer
1H NMR (500MHz) spectrum of purified cyclic dimer of 12-HSA in CDCl3.
a
a
b
b
c
c
d
d
e
e
f
f
c
b
a
f
b
b
c
c
d
e
a
b
c, d
e
f
g
1H NMR (200MHz) spectrum of p(12-HSA) in CDCl3.
1H-NMR of Poly(12-HSA)
ROP of cyclic dimer of 12-HSA was confirmed by the opening of ring by the appearance of peak at 3.59 ppm
1H NMR (500MHz) spectrum of vacuum distilled Me12-HS in CDCl3.
a
a
b
b
c
c
d
d
e
e
f
f
c
b
g
g
Unsaturation
absent
DP vs time
The rate of polymerization, as evidenced by the change of DP with time, indicates that the rate is faster with a titanium based catalyst at both temperatures.
1H-NMR of Me 12-HS
Absence of unsaturation and the ratio of g/f/e peak is 3:1:2, indicates this is an AB monomer.
MALDI-TOF of Poly(Me 12-HS)
12-hydroxystearic acid (12-HSA) is a biorenewable AB monomer and is readily available from castor seed oil.
However, commercial 12-HSA contains several monofunctional impurities which can act as chain terminator. It is not surprising, therefore, there is only one report of polymers derived from 12-HSA (Poly(12-HSA)) with reasonably high molecular weights1.
Long aliphatic segments in polyesters provide significant opportunity for enahancement of crystallinity2. However, the hexyl side chain in a polymer derived from 12-HSA is likely to inhibit crystallization.
We have explored the use of purified methyl 12-hydroxy stearate (Me 12-HS) as an AB monomer for polymerization by transesterification-polycondensation (TE-PC) using suitable catalysts.