## Slide 1
High molecular weight poly (L-(+)-lactic acid)s are generally prepared by ROP of cyclic dimer, L-lactide, which is a crystalline solid. This involves conversion of an aqueous solution of L-lactic acid to a dimer, followed by its purification and polymerization.
It would be desirable to have a non aqueous precursor to poly(L-lactic acid), which is relatively less volatile and is capable of efficient step growth polymerization.
Simple alkyl esters of L-(+)-Lactic acid are not very useful because of their high volatility under conditions normally employed for step growth reactions.
Such a monomer or precursor will also enable synthesis of copolymers of L-lactic acid/esters with α, ω-hydroxyl ester compounds, many of which are naturally available.
Mr. Yogesh Nevare is thankful to DST, New Delhi for financial support.
The assistance of Dr. P. R. Rajamohanan, CSIR-NCL for NMR analysis is gratefully acknowledged.
Objectives
Synthesis
Acknowledgement
High molecular weight Poly(L-Lactic acid)s and their copolymers by polycondensation: Is it Possible ?
Yogesh R. Nevare, Bhaskar B. Idage, Susheela B. Idage, Swaminathan Sivaram*
Polymer Science and Engineering Division,
National Chemical Laboratory, Pune – 411 008
Email: s.sivaram@ncl.res.in; yr.nevare@ncl.res.in
Structure and composition of 1
Structure and composition of 3
Tg
Tc
Tm
Future work
DSC thermogram of 4.
Structure and composition of 4
MALDI-TOF-MS spectra of 4.
1H NMR Spectrum of 4 in DMSO-d6.
M. Vert et. al.; Macromolecules, 29, 3535 (1996).
1H NMR Spectrum of 1 in DMSO-d6.
Structure and composition of 2
1H NMR Spectrum of 2 in DMSO-d6 .
1H NMR Spectrum of 3 in DMSO-d6 (DP= 4.75).
14mer
15mer
16mer
17mer
18mer
19mer
20mer
21mer
22mer
23mer
24mer
25mer
26mer
27mer
28mer
29mer
30mer
31mer
34mer
35mer
8mer
41mer
43mer
4mer
5mer
6mer
7mer
8mer
9mer
10mer
11mer
12mer
13mer
m/z
m/z
a
b
c, f, j
d, g
h, i, e
b
d, g
e
h, i
a
b
c, f, j
d, g
e
h, i
b
d, g
e
h, i
a’
c’ f’ j’
b’
d’ g’
e’
h’ i’
k’
b’
d’ g’
h’ i’ e’
k’
c’ f’ j’
b’
d’ g’
h’ i’ e’
k’
b’
d’ g’
h’ i’ e’
k’
To examine the kinetics of transesterification Vs cyclic dimer formation using 3 as the precursor and comparison with polymerization of aqueous L-lactic acid.
To establish the structure of polymers in terms of composition and end groups.
To examine the effect of structural variation of 3 as relative rates of chain growth and cyclization.
Synthesis of a novel AB precursor for preparation of Poly(l-lactic acid ester)s.
Aqueous L-(+)-lactic acid can be extracted into a CH2Cl2 solution. The organic solution of L-(+)-lactic acid has DP= 1.76.
L-(+)-lactic acid, commercial procured, is a mixture of monomer and higher oligomers with an DP=1.45.
Formation of the AB precursor with a DP= 2.33 which confirming the addition of 1 methyl lactate unit.
AB precursor 3 undergoes further chain extension under step growth polymerization conditions. However, this is accompanied with the formation of ~ 20 % L-lactide 5.